Ultrapolymers adds TRIREX® polycarbonates from Samyang to its portfolio

Applications for the new TRIREX® polycarbonates from Samyang that now form part of the Ultrapolymers portfolio extend from highly transparent automotive parts to housings for consumer and household electronics, and containers such as beakers and food storage boxes.

Augsburg/Germany, April 2016. Plastics distributor Ultrapolymers Deutschland (www.ultrapolymers.com) has extended its portfolio of engineering plastics by adding the standard TRIREX® polycarbonate grades from Samyang Corporation (www.samyangcorp.com). Their viscosities (MFI 300 °C, 1.2 kg) range from 34 g/10 min with the ultra-easy-flow 3017 grades for thin-wall injection moulding to 3 g/10 min with the high-viscosity 3030 extrusion grades. Depending on the application, special additives can be incorporated, for example to increase the heat and/or UV stability. Optical quality grades are also available. All the TRIREX® standard grades are classified to UL94 in flammability Class V-2 at 1.5 mm and comply with the requirements of the EU and FDA for food-contact applications.

Thanks to their high transparency, dimensional stability, impact strength and temperature resistance and their very good mechanical and dielectric properties, TRIREX® PC types are suitable for a wide variety of applications, including housings for electrical and electronic devices, automotive lamps, plug connectors, optical components and containers for industry, trade and the home. Ultrapolymers markets the TRIREX® PC types in Germany, Austria and Switzerland.

TRIREX® is a brand of the Samyang Corporation.

Ultrapolymers Deutschland GmbH, Augsburg/Germany, supplies customers in Germany and Switzerland and is part of the pan-European plastics distributor Ultrapolymers Group NV, Lommel/Belgium. Headquartered in Augsburg, Ultrapolymers Deutschland has sales offices in Bielefeld, Kierspe, Nuremberg, and Stuttgart. Austrian customers are looked after by Ultrapolymers Austria GmbH, Werndorf/Austria.

The company’s portfolio includes polyolefins from LyondellBasell, polystyrene and ABS from Styrolution, polyamide from Ascend, Domo and Ravago, polycarbonate from Samyang, synthetic rubbers from LANXESS, long-fibre reinforced thermoplastics, TPU from Ravago, bio-based polymers from FKuR, rotational moulding polymers from LyondellBasell, commodities, masterbatches and additives, the Colorflexx service package for the self-colouring of ABS as well as customer-specific compounds.

Voucher copies and editorial contact:
Konsens PR GmbH & Co. KG, Dr. Jörg Wolters
Hans-Kudlich-Str. 25, D-64823 Groß-Umstadt
Tel.: +49 (0) 60 78/93 63-13, Fax: +49 (0) 60 78/93 63-20
E-Mail: mail@konsens.de

Please find this press release as Word file and the high-resolution image for download under: http://www.konsens.de/ultrapolymers.html